## Slide 1
Sepideh Kavousi Department of Mechanical Engineering & Materials Science Program
Colorado School of Mines
ZaeemLab.com
Supervised linear regression machine learning model to predict the primary dendritic arm spacing

## Slide 2
Problem Statement
2
Hunt-Burden (HB) model
Kurz-Fisher (KF) model
Computational PDAS versus analytical models for Si-9at.%As 1
Analytical Models predicting Primary Dendritic Arm Spacing (PDAS)
Analytical relations for PDAS have significant deviations from computational predications and experimental data
1 https://doi.org/10.1016/j.actamat.2020.116562
Experimental PDAS versus analytical models for Al-11Si 2
2 https://doi.org/10.3390/met8100784

## Slide 3
Workflow
3
FCC system: Ti-X at% Ni ( X=3.4, 7.1, 10.7)
HCP system: Mg-9 at%Al
BCC system: Al-X at%Cu (X=6,8,10)

## Slide 4
The Computational Data
4
 | V (m/s) | G (K/m) | Number of data points from PF modeling
Ti-3.4 at% Ni | 0.01-0.09 | 107, 8×106, 7×106, 6×106, 5×106 | 45
Ti-7.1 at% Ni | 0.01-0.09 | 107, 8×106, 7×106, 6×106, 5×106 | 42
Ti-10.4 at% Ni | 0.0001-0.02 | 107, 5×106 | 22
Mg-9 at% Al | 0.005-0.12 | 5×106, 3×106, 1×106 | 21
Al-6 at% Cu | 0.001-0.06 | 107, 8×106, 7×106, 6×106, 5×106 | 47
Al-8 at% Cu | 0.01-0.08 | 107, 8×106, 7×106, 6×106, 5×106 | 43
Al-10 at% Cu | 0.008-0.005 | 107, 8×106, 7×106, 6×106 | 30

## Slide 5
ML model
5
HB model
KF model
KF model
HB model

## Slide 6
Supervised Machine Learning Linear Regression Model
6
HB model

## Slide 7
Supervised Machine Learning Linear Regression Model
7
KF model
7
2
7

## Slide 8
Supervised Machine Learning Linear Regression Model
8

## Slide 9
Conclusion
9
In this project we develop a supervised-regression machine learning model to obtain a correlation between the PDAS and velocity and temperature gradient
We obtain a very important conclusion that in contract to analytical models, where temperature gradient plays much important role in the PDAS estimations, the velocity and temperature play almost equal roles in PDAS correlation!
Fitting the data for the individual alloys were not helpful because we did not put any restriction on how the material properties equation looks like and therefore alpha and beta values seem all around the place

## Slide 10
Recommendation
10
The material scientists are recommended to use the modified-HB and modified-KF models instead of the original analytical HB and KF models.
HB model
KF model
Modified HB model
Modified KF model